GL FORM 3: GEAR LUBRICANT LABORATORY PERFORMANCE RESULTS

| I. | Oil Company: |  | Date: |  | Meeting/Program: |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Specification: |  | Viscosity Grade: |  | Formula No.: |  |
|  | Company: |  | Brand Name: |  |

| Test Identification | Test Results | Committee Recommendation |
| --- | --- | --- |
| Test: | D 7038 | ASTM Rating: |  |  |  |
| Date: |  | Area | Rust Level | Area | Rust Level |  |  |
| Lab: |  | 1 |  | 6 |  |  |  |
| Gear Batch: |  | 2 |  | 7 |  |  |  |
|  |  | 3 |  | 8 |  |  |  |
| Test No.: |  | 4 |  | 9 |  |  |  |
|  |  | 5 |  | 10 |  |  | A: |  |  | NA: |  |  |
| Test: | D6121 (noncoated) | ASTM Rating: |  |  |
| Date: |  | Ratings | Ring |  | Pinion |  |
| Lab: |  | Ridging: |  |  |  |  |
| Gear Batch: |  | Rippling |  |  |  |  |
| Test No.: |  | Wear: |  |  |  |  |
|  |  | Scoring: |  |  |  |  |
|  | Pitting/Spalling: |  |  |  |  |
|  | Remarks: |  | A: |  |  | NA: |  |  |
| Test: | D6121 (coated) | ASTM Rating: |  |  |
| Date: |  | Ratings | Ring |  | Pinion |  |
| Lab: |  | Ridging: |  |  |  |  |
| Gear Batch: |  | Rippling |  |  |  |  |
| Test No.: |  | Wear: |  |  |  |  |
|  |  | Scoring: |  |  |  |  |
|  | Pitting/Spalling: |  |  |  | A: |  |  | NA: |  |  |
|  | Remarks: |  |  |
| Test: | L-42 | Ring: | % Score |  | Pinion: | % Score |  |  |
| Date: |  | D: |  |  |  |  | D: |  |  |  |  |
| Lab: |  | C: |  |  |  |  | C: |  |  |  |  |
| Gear Batch: |  | Comments: | A: |  |  | NA: |  |  |
| Test No.: _______________ |  |  |
| Test: | L-42 (2nd)* | Ring: | % Score |  | Pinion: | % Score |  |  |
| Date: |  | D: |  |  |  |  | D: |  |  |  |  |
| Lab: |  | C: |  |  |  |  | C: |  |  |  |  |
| Gear Batch: |  | Comments: | A: |  |  | NA: |  |  |
| Test No.: _______________ |  |  |

| Comments: |  |
| --- | --- |

19-NOV-12